厦门斯玛克进出口有限公司

No:(2005)SM01

###### Inspection Reports

Product Name: Tapered Roller Bearing

# Type: HM218248/HM218210

Applicant: xxx  BEARING FACTORY

## NOTICE

- The inspection reports would be invalid without stamp for inspection report.

- The copy of inspection reports would be invalid without added inspection report or inspection unit stamp.

- The inspection report would be invalid without signatures.

- The inspection report would be invalid if altered.

- If there is any objection to the inspection reports, please claim to inspection unit in 15days.Any claim later than 15 days will not be considered.

- The inspection data is only valid to the samples.

Add: RM#1902, NO.584,DEXIN BUILDING,XIANYUE ROAD,XIAMEN, CHINA

Post Code:361004

Tel:(86)(592)6780643

Fax:(86)(592)6106330

厦门斯玛克进出口有限公司

Page 1 of 3

| Report Number | (2005)SM01 | Product Name | Tapered Roller Bearing |
| --- | --- | --- | --- |
| Type | HM218248/HM218210 | Inspection Type | Entrusted Test |
| Client | xxx factory |  |  |
| Address |  |  |  |
| Brand |  | Post Code |  |
| Contour Dimension | 89.974×146.975×40 | Sampling Pattern | Deliver sample |
| Accuracy Grade | P0 | Sampling Place | Storehouse |
| Material | GCr15 | Sampling Base | 10000units |
| Production Date | 12/2004 | Sampling Quantity | 5 units |
| Inspection Date | 1/2005 | Sampling Date | 1/2005 |
| Inspection Place | Lab for Testing Reliability&Life | Sample Supplier |  |
| Inspection Standards | JB/T50013，P-VW2006 |  |  |
| Inspection Conclusion | The synthetic identification is that the sample life attain eligible,K=1, with 90% reliability. (Stamp for inspection report) Date of issue: |  |  |
| Remark |  |  |  |

Approving By:                  Verifier By:                 Compiler By:

厦门斯玛克进出口有限公司

Page 2 of 3

| Client: xxx factory Type: HM218248/HM218210 Accuracy Grade: P0 Report No:(2005)SM01 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Test Method | Truncation Test |  | Sample Quantity |  | 4 Units |  |
| Test Condition | Equivalent dynamic load/ Basic dynamic load rating （P/ C） |  | 0.499 |  |  |  |
|  | Radial load (Fr) |  | / N |  |  |  |
|  | Axial load (Fa) |  | 62500 N |  |  |  |
|  | Rotating speed of test (n) |  | 1800 r/min |  |  |  |
|  | Basic rating life (L10) |  | 94 h |  |  |  |
|  | Lubrication and cooling |  | Circulating lubrication by N32 oil |  |  |  |
| Test Conclusion | 1. Initial data of test in page 3 of 3 |  |  |  |  |  |
|  | 2. Data treatment conclusion： Experimental value of basic rating life L10t = 187 h Ratio of life : K= 1 Reliability of L10: Re = 90 % |  |  |  |  |  |
| Test Start Date： |  | 1/2005 |  | Test End Date： |  | 1/2005 |

厦门斯玛克进出口有限公司

- Page 3 of 3

| Client: xxx factory Type: HM218248/HM218210 Accuracy Grade: P0 Report No:(2005)SM01 |  |  |  |  |
| --- | --- | --- | --- | --- |
| No. | Sample No. | Running time（h） | Damaged parts | Remarks |
| 1 | （2005）SM01-1 | 187 |  | Time,stop test |
| 2 | （2005）SM01-2 | 187 |  | Time,stop test |
| 3 | （2005）SM01-3 | 187 |  | Time,stop test |
| 4 | （2005）SM01-4 | 187 |  | Time,stop test |
| 5 |  |  |  |  |
| 6 |  |  |  |  |
| 7 |  |  |  |  |
| 8 |  |  |  |  |
| 9 |  |  |  |  |
| 10 |  |  |  |  |
| 11 |  |  |  |  |
| 12 |  |  |  |  |
| 13 |  |  |  |  |
| 14 |  |  |  |  |
| 15 |  |  |  |  |
| 16 |  |  |  |  |
| 17 |  |  |  |  |
| 18 |  |  |  |  |
| 19 |  |  |  |  |
| 20 |  |  |  |  |