厦门斯玛克进出口有限公司

No:(2006)LW01

###### Inspection Reports

Product Name: 密封深沟 Bearing

# Type: 6204-2RS

Applicant: xxx  BEARING FACTORY

## NOTICE

- The inspection reports would be invalid without stamp for inspection report.

- The copy of inspection reports would be invalid without added inspection report or inspection unit stamp.

- The inspection report would be invalid without signatures.

- The inspection report would be invalid if altered.

- If there is any objection to the inspection reports, please claim to inspection unit in 15days.Any claim later than 15 days will not be considered.

- The inspection data is only valid to the samples.

Add: RM#1902, NO.584,DEXIN BUILDING,XIANYUE ROAD,XIAMEN, CHINA

Post Code:361004

Tel:(86)(592)6780643

Fax:(86)(592)6106330

厦门斯玛克进出口有限公司

检   验   报  告   结  论

共4页  第1页

| 报告编号 | NO:LW-2006-001 | 产品名称 | 深沟球轴承 |
| --- | --- | --- | --- |
| 型号规格 | 6204-2RS | 检验类别 | 委托检验 |
| 受检单位 |  | 详细地址 |  |
| 商标 |  | 抽样方式 |  |
| 外形尺寸 | 20×47×14 | 抽样地点 |  |
| 公差等级 | P0 | 抽样基数 |  |
| 材质 | GCr15 | 抽样日期 |  |
| 生产日期 |  | 抽样日期 |  |
| 检验日期 | 2006-2-8 | 抽样者 |  |
| 检验地点 | 动态实验室 | 检验依据 | JB/T8571-1997 |
| 检 验 结 论 | 综合判定本批样品为合格品. 检验报告专用章 签发日期 2006 年 2 月 30 日 |  |  |
| 附 注 |  |  |  |

批准:                                  审核:                          编制:

厦门斯玛克进出口有限公司

轴承漏脂、温升检验报告

共4页  第2页

| 受检单位: 厦门斯玛克进出口有限公司 规格型号: 6204-2RS 公差等级: P0 报告编号: LW-2006-001 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 试 验 方 法 |  |  |  | 样本容量 |  |  | 16套 |
| 试 验 条 件 | 试验机型号 |  | TSG10-60n |  |  |  |  |
|  | 径向负荷(Fr) |  | 196 N |  |  |  |  |
|  | 轴向负荷(Fa) |  | / N |  |  |  |  |
|  | 试验转速(n) |  | 漏脂 |  | 2700 r/min |  |  |
|  |  |  | 温升 |  | 6750 r/min |  |  |
|  | 试验时间 |  | 6 h |  |  |  |  |
|  | 润滑 |  | 原装脂 |  |  |  |  |
| 仪 器 仪 表 | 转速 |  | 变频器 |  |  |  |  |
|  | 温度 |  | 温度传感器 |  |  |  |  |
|  | 称重 |  | 精密电子天平 精度≤0.001g |  |  |  |  |
| 试验开始日期 |  | 2006 年2月 8日 | 试验结束日期 |  |  | 2006年 2 月20 日 |  |

厦门斯玛克进出口有限公司

轴承漏脂试验数据

共4页  第3页

| 受检单位: 厦门斯玛克进出口有限公司 规格型号: 6204-2RS 公差等级: P0 报告编号: LW-2006-001 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 序号 | 样品编号 | 扭矩 (in-oz) | 温升 (℃) | 漏脂率(%) | 标准值 (%) | 是否 合格 | 备注 |
| 1 | L001-1 | 2.0 | 26.3 | 0.4 | ＜5 | 合格 |  |
| 2 | L001-2 | 1.8 | 25.9 | 0 |  | 合格 |  |
| 3 | L001-3 | 1.4 | 22.9 | 2.0 |  | 合格 |  |
| 4 | L001-4 | 1.9 | 23.7 | 0.1 |  | 合格 |  |
| 5 | L001-5 | 1.9 | 21.8 | 0.1 |  | 合格 |  |
| 6 | L001-6 | 1.5 | 23.7 | 0.3 |  | 合格 |  |
| 7 | L001-7 | 1.5 | 26 | 5.5 |  | 不合格 | 外圈漏脂 |
| 8 | L001-8 | 1.9 | 28 | 0 |  | 合格 |  |
| 9 |  | 以下空白 |  |  |  |  |  |
| 10 |  |  |  |  |  |  |  |
| 11 |  |  |  |  |  |  |  |
| 12 |  |  |  |  |  |  |  |
| 13 |  |  |  |  |  |  |  |
| 14 |  |  |  |  |  |  |  |
| 15 |  |  |  |  |  |  |  |
| 16 |  |  |  |  |  |  |  |
| 试验结果 |  | 合格样品数 |  | 7套 |  |  |  |
|  |  | 不合格样品数 |  | 1套 |  |  |  |

厦门斯玛克进出口有限公司

轴承温升试验数据

共4页  第4页

| 受检单位: 厦门斯玛克进出口有限公司 规格型号: 6204-2RS 公差等级: P0 报告编号: LW-2006-001 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 序号 | 样品编号 | 扭矩 (in-oz) | 温升 (℃) | 漏脂率(%) | 标准值 (℃) | 是否 合格 | 备注 |
| 1 | W002-1 | 1.0 | 36.3 | 0.4 | ＜55 | 合格 |  |
| 2 | W002-2 | 1.8 | 35.9 | 0 |  | 合格 |  |
| 3 | W002-3 | 1.4 | 42.9 | 2.0 |  | 合格 |  |
| 4 | W002-4 | 1.9 | 43.7 | 0.1 |  | 合格 |  |
| 5 | W002-5 | 1.1 | 31.8 | 0.1 |  | 合格 |  |
| 6 | W002-6 | 1.5 | 33.7 | 0.3 |  | 合格 |  |
| 7 | W002-7 | 1.5 | 40 | 5.5 |  | 合格 |  |
| 8 | W002-8 | 1.9 | 38 | 0 |  | 合格 |  |
| 9 |  | 以下空白 |  |  |  |  |  |
| 10 |  |  |  |  |  |  |  |
| 11 |  |  |  |  |  |  |  |
| 12 |  |  |  |  |  |  |  |
| 13 |  |  |  |  |  |  |  |
| 14 |  |  |  |  |  |  |  |
| 15 |  |  |  |  |  |  |  |
| 试验结果 |  | 合格样品数 |  | 8套 |  |  |  |
|  |  | 不合格样品数 |  | 0套 |  |  |  |